Search for New n-type Thermoelectric Cobalt Oxides

S. Hébert, D. Flahaut, V. Caignaert, C. Martin, D. Pelloquin and A. Maignan

Laboratoire CRISMAT, UMR6508, ENSICAEN

6Bd du Maréchal Juin, 14050 Caen Cedex, France

sylvie.hebert@ismra.fr

The potential application of oxides as thermoelectric elements used for high temperature application has first been demonstrated by Terasaki et al. [1] in NaxCoO2. The coexistence of a small resistivity together with a large thermopower and a small thermal conductivity makes NaxCoO2 a good example of a ‘phonon glass and electron crystal’ [2]. The peculiar transport properties in this oxide are mainly linked to the presence of CoO2 layers corresponding to a layer of tilted edge-shared CoO6 octahedra. In the CoO2 layers, a mixture of Co3+ and Co4+ is responsible for the metallicity and might be responsible for the large thermopower [3].

Following this study, the transport properties of a related family, the misfit cobalt oxides have been investigated by several groups [4, 5]. In this family, CoO2 layers similar to the ones in NaxCoO2 are separated by NaCl-like layers. By different substitutions, promising results have been obtained for p-type thermoelements [6]. Even though many different kinds of substitution have been attempted in these materials to dope them with electrons, n-type misfit materials are still lacking.

The richness of the cobalt oxides is due to the different valence states (Co2+, Co3+ and Co4+) and spin states (Low, Intermediate or High spin states) that can be found depending on the structure. To find new n-type thermoelectric oxides, we have investigated different structures of cobalt oxides apart from the misfit structure. The 3D perovskite LaCoO3 is insulating and exhibits a large and positive thermopower. By doping with only a few percent of tetravalent cations such as Ce4+ or Th4+, a spectacular change of sign of the Seebeck coefficient can be induced, from +600 to –300V/K at 300K. The thermal conductivity is small, less than 2Wm-1K-1. The resistivity is slightly smaller in the substituted samples than in the undoped one, reaching 1.cm at 300K and is decreasing with temperature [7]. Such kind of substitution is thus a powerful way to induce n-type oxides. Similarly, substitutions are now attempted in other cobaltites to induce Co2+ in the Co3+ matrix. We will present results in the 1D Ca3Co2O6 chains as well as in the 112 YBaCo2O5+x compounds.

[1] : I. Terasaki, Y. Sasago, K. Uchinokura, Phys. Rev. B 56, R12685 (1997).

[2] : K. Takahata, Y. Iguchi, D. Tanaka, T. Itoh, I. Terasaki, Phys. Rev. B 61, 12551 (2000).

[3] : W. Koshibae, K. Tsutsui, S. Maekawa, Phys. Rev. B 62, 6869 (2000).

[4] : A. C. Masset, C. Michel, A. Maignan, M. Hervieu, O. Toulemonde, F. Studer, B. Raveau, J. Hejtmanek, Phys. Rev. B 62, 166 (2000).

[5] : R. Funahashi, I. Matsubara, S. Sodeoka, Appl. Phys. Lett. 76, 2385 (2000).

[6] : A. Maignan, S. Hébert, D. Pelloquin, C. Michel, J. Hejtmanek, J. Appl. Phys. 92, 1964 (2002).

[7] : D. Flahaut, S. Hébert, A. Maignan, submitted to Eur. Phys. J.B