Effective Mass and Mobility in р-Bi2-xSbxTe3-ySey Solid Solutions below Room Temperature Range

### L.N. Luk’yanova, V.A. Kutasov, and P.P. Konstantinov

Ioffe Physical-Technical Institute, Russian Academy of Sciences, St.-Petersburg, 194021 Russia

###### Email: lidia.lukyanova@mail.ioffe.ru

Thermopower coefficient () and electrical conductivity () of the multicomponent р-Bi2-xSbxTe3-ySey solid solutions based on bismuth and antimony chalcogenides with substitutions of atoms in cationic (1x1.3) and anionic (0.04y 0.09) sublattices of bismuth telluride were studied in the temperature range (80К-340К).

In the low-temperature interval 80К-150К, the temperature dependence of the effective mass (m/m0) was found to be weaker in all compositions of the р-Bi2-xSbxTe3-ySey solid solutions studied. With growth of temperature more than 150К the effective mass (m/m0) increases due to non-parabolisity of valence band. A maximum slope dln (m/m0)/dlnT was obtained for solid solution at х=1.3. For the same solid solution a slope of the temperature dependence of the mobility dln μ0/dlnT increases in the range (150К>T>220К) comparing with composition with smaller contents of Sb-atoms. Such peculiarities in the effective mass and the mobility leads to growth of the thermoelectric efficiency (Z) through the interval 150К-220К.

At the temperatures lower than 150 K the growth of Z is expected for the solid solutions with smaller contents of Sb (х = 1.2) and with higher slope the effective mass and the mobility at these temperatures.

Thus, the study performed allows, that alteration of the effective mass (m/m0) and the mobility (μ0) dependences on temperature and composition of the р-Bi2-xSbxTe3-ySey solid solution determines the increase of the thermoelectric efficiency (Z).

The work is supported by the project RFBR N03-02-17605а.

Presentation Preference: Poster

The corresponding author:

Ph. D. Lidia. N. Luk'yanova, senior researcher

Ioffe Physical-Technical Institute, Russian Academy of Sciences,

Polytekhnicheskaya 26, St. Petersburg, 194021 Russia

Phone: (7) 812 5159247

Email: lidia.lukyanova@mail.ioffe.ru