Influence of Phase Composition on Thermoelectric Performance of CoSb3 Skutterudites

- C. Stiewe1, M. Toprak2, D. Platzek1, E. Müller1, M. Muhammed2

1 German Aerospace Center (DLR), Inst. of Materials Research, D-51170 Cologne, Germany

2 Royal Institute of Technology, Materials Chemistry Division, SE-10044 Stockholm, Sweden

Recently, nano-structured Skutterudite materials have been prepared following a newly developed route of chemical co-precipitation [1]. This technique has the advantage of relatively low preparation temperatures compared to conventional metallurgical methods, thus retaining the nano-structure of small-grained powders. Furthermore, the low process temperature makes this technique more attractive for industrial use because of shorter time consumption for preparation and easier upscaling.

Up to now highest figure of merit was measured among Skutterudite samples with a certain level of Nickel substitution for Cobalt and of Tellurium substituting Antimony, respectively [2].

A specific phase composition of CoSb3, CoSb2 and Sb was observed in these samples by means of powder X-ray diffraction (XRD) followed by Rietveld refinement. This composite showed up to have better thermoelectric properties than single-phase CoSb3.

In order to get a better insight of how the phase composition affects the TE properties, a series of Ni- and Te-doped CoSb3 samples with various percentage of phase impurities have been prepared, characterized and evaluated with respect to their electrical and thermal conductivity, and Seebeck coefficient.

Results of these measurements and XRD characterization are presented along with an analysis of the CoSb2 influence on the structure and transport characteristics.

[1]	Bertini, L., C. Stiewe, M. Toprak, S. Williams, D. Platzek, Y. Zhang, C. Gatti, E. Müller, M. Muhammed, and M. Rowe, Nanostructured Co1-xNixSb3 Skutterudites: Synthesis, Thermoelectric Properties, and Theoretical Modeling, Journal of Applied Physics, 2003. 93 (1), pp. 438-447.

[2]	Bertini, L., K. Billquist, M. Christensen, C. Gatti, L. Holmgren, B. Iversen, E. Müller, M. Muhammed, G. Noriega, A. Palmqvist, D. Platzek, D.M. Rowe, A. Saramat, C. Stiewe, M. Toprak, S.G. Williams, and Y. Zhang, Thermoelectric Properties of Nano-Grained CoSb3 Skutterudites Doped with Ni and Te, in Proc. 22nd International Conference on Thermoelectrics 2003, La Grande Motte, France, IEEE Piscataway 2004, pp. 48-51.

Oral preferred