# TRANSITION A SEMICONDUCTOR – SEMIMETAL IN NANOWIRES Bi1-XSbX INDUCED BY ELASTIC EXPANSION

A.A. Nikolaeva1, 3, D.V. Gitsu1, T.E. Huber2, L. A. Konopko1,3, I. Popov 1

1Institute of Applied Physics, Academy of Sciences of Moldova, MD-2028, Academy str. 5, Chisinau, MD-2028, Moldova

2Department of Chemistry, Howard University, DC 20059, 525 College St. N.W. Washington, USA

3International Laboratory of High Magnetic Fields and Low Temperatures, Wroclaw, Poland

The work is devoted to investigation of the thermo and magnetothermoelectric properties of single Bi1-xSbx  nanowires (200nm < d < 5µm) in glass coating under the elastic deformation up to =2.5% relative elongation in the temperature range 4.2-300K and magnetic field up to 14T.

Nanowires Bi-6at%Sb, Bi-8at%Sb in the not deformed condition are semiconductors with a narrow energetic gap Eg ~ 4meV. For want of elastic expansion of wires the gradual bonding of a sample happens, the resistance decreases more than in 2 times and for want of some significance к the transition a semiconductor - semimetal happens. The transition was precisely registered with the help of Shubnikov de Haas oscillations. On longitudinal magnito resistance and magnito thermopower such transition is a special case of electronic topological transition Lifshits and is accompanied by anomaly on thermopower near to a transition point. This anomaly was registered and was investigated with the help of curves deformation of   thermopower for want of various temperatures. Calculated up Power factor α2s (where α - thermopower, and - conductivity) depending on temperature, diameter of wires, magnetic field and expansion.

The work was stimulated by  that now conductors Bi1-xSbx are the best thermoelectric material for n- of a branch for want of 80-100К. Per the last years the large attention is given to quantum wires of Bi and Bi-Sb. The increase of thermoelectric efficiency Z=α2/α in some times due to quantum dimensional effect would be predicted. As a matter of fact, the elastic expansion of wires because of Bi1-xSbx allows to investigate electrical and thermoelectric properties for want of continuously varying gap Eg and by that to evaluate theoretical development concerning increases Z with a modification of a gap Eg.

The work was supported by the Civilian Research Defense Corporation, CGP- grant  # MO-E1-2603-SI-04.