Structural and thermoelectric properties of undoped IV-VI epitaxial films alloyed with tin

- J. Nurnus, H. Böttner, R. Glatthaar, J. König, A. Lambrecht

Fraunhofer-Institut für Physikalische Messtechnik (IPM), Heidenhofstraße 8, D-79110 Freiburg, Germany

IV-VI-compounds are well known materials with favourable thermoelectric properties at elevated temperatures (~700 K). Using related mixed crystals the thermoelectric properties can be optimized due to alloy scattering which leads to a decrease of the thermal conductivity without changing the other thermoelectric properties significantly. This method is well known as Joffe concept. The Joffe concept is about 50 years old and successfully proved several times using bulk crystals. But only few data exist about semiconductor thin films. Here we report on structural (SEM-, EDX-, XRD-, FT-IR-analysis) and in particular thermoelectric properties (Seebeck coefficient and Hall-Effect measurements for carrier concentration, conductivity and mobility) of molecular beam epitaxy grown thin film based on the "Joffe-systems" (Pb,Sn)Se and (Pb,Sn)Te. Special care was taken to evaluate the in-plane thermal conductivity of insulated free standing (Pb,Sn)Se thin films.

With increasing tin concentrations increasing charge carrier concentration as well as increasing thermopower values were observed. The bandgap decreased with increasing tin concentration – shifting the optimum operating temperatures towards room temperature – and also the lattice thermal conductivity decreased as expected due to alloy scattering. All these effects strongly improve the thermoelectric properties of Sn-alloyed IV-VI epitaxial layers in the room temperature region.

Technical Topic Category: Thermoelectric materials

- Presentation preference: Oral

- Presenting author: Dr. A. Lambrecht

- Contact author: Dr. J. Nurnus

Fraunhofer Institute for Physical Measurement Techniques
Heidenhofstr. 8
79110 Freiburg/Breisgau
Germany

Phone: 49 / 761/8857-124
Fax: 49 / 761/8857-224
E-mail: joachim.nurnus@ipm.fraunhofer.de