Thermopower in La1-xCexB6 Kondo systems

V.H.Vardanyan1, S.R. Harutyunyan1 ,V.R. Nikoghosyan1, A.S. Kuzanyan1,

K.S. Wood2, A.M. Gulian3, S. Kunii4 and K. Winzer5.

1Institute for Physical Research NAS, Ashtarak, 378410, Armenia

2NRL, Washington, DC 20375, USA

3PAF/NRL, Washington, DC 20375, USA

4Department of Physics, Tohoku University, Sendai, Japan

5Universität Göttingen, Germany.

# The temperature dependence (4-300 K) of the thermopower of Kondo system

# La1-xCexB6 has been measured. The thermopower of CeB6(x=1) shows Kondo peak at temperature ~ 10 K. The decreasing the value of the peak and the shift of this peak to the lower temperature for the concentration of Ce (x=0.1, 0.05, 0.03) has been observed. In addition, for the concentration of Ce (x=0.02, 0.005, 0.0025) the plateau at around 15 K has been observed.