Properties of the Electron and Phonon Sub-systems of Tin-doped Bismuth Telluride-based Solid Solutions

- M. K. Zhitinskaya1, S. A. Nemov1, M. Yu. Nikulina1,

- T. E. Svechnikova2, E. Müller3, D. Platzek3

- State Polytechnical University, St. Petersburg, Russia

- Baikov Institute of Metallurgy and Materials Sciences, Moscow, Russia

- German Aerospace Center (DLR), Institute of Materials Research, Köln, Germany

We report the results of an experimental study of the Nernst-Ettingshausen and other basic transport coefficients: electrical and thermal conductivity, Hall and Seebeck coefficients and their anisotropy in Bi2-xSnxTe3-ySey single crystals doped with Sn. All crystalls were grown by the Czochralski technique. The p-type samples show similar peculiarities in the temperature dependence of the transport coefficients that can be explained by the presence of resonant states of Sn. Improved thermoelectric properties of n-type Bi2-xSnxTe3-ySey were found: a maximum of Z = 3.3∙10-3 K-1 at 340-370 K which is a larger value compared to solid solutions without Sn. We observed a different influence of Sn atoms on the electron and phonon sub-systems: an increase of the thermal resistivity, whereas the electron mobility doesn’t change simultaneously. Moreover, improved homogeneity of the carrier concentration distribution was detected by locally resolving measurement of the Seebeck coefficient by the scanning thermo-probe on these crystals.

The obtained experimental data support to the point of view that the incorporation of Sn atoms into Bi2Te3-xSex is accompanied by the formation of a band of Sn states against the background of the allowed valence-band spectrum that interact with basic electron states of these compounds.